SMART FORMULATOR  |  TASK 1 — PROPERTY GLOSSARY

Supplier-datasheet recognition guide  •  Record stated facts only; retain unit, temperature, method, value type, document and page.

Color key: Tier 1 = blocking (red), Tier 2 = verifies the finished oil (amber), Tier 3 = justifies a substitution (blue). Component rows: All / VM / PPD.

A  BASE OILS — Tier 1 blocking / Tier 2 verification / Tier 3 substitution

| Tier | Property / field | Meaning | Unit / test condition |
| --- | --- | --- | --- |
| 1 | API group / chemistry | Base-stock classification (I–V) and oil family. | Category; mineral, PAO, ester, etc. |
| 1 | KV40 / KV100 | Kinematic viscosity at two reference temperatures. | cSt (= mm²/s); 40°C / 100°C |
| 1 | Viscosity index (VI) | Index of viscosity change with temperature. | Unitless; derived from KV40/KV100 |
| 1 | Density | Mass per unit volume of oil. | kg/m³; record reference °C (often 15°C) |
| 1 | CCS | Cold-cranking apparent viscosity. | mPa·s; stated subzero °C |
| 2 | MRV / yield stress | Low-temperature pumping viscosity / stress to initiate flow. | mPa·s / Pa; stated subzero °C |
| 2 | Noack volatility | Mass fraction evaporated in a specified test. Records use only a source-stated test temperature, else null. | wt.% loss; standard 250°C for 1 h |
| 2 | Pour / flash point | Low-temperature flow limit / vapor ignition temperature. | °C; flash test method COC or PMCC |
| 3 | Sulfur / saturates / aromatics | Composition markers used in base-oil comparison. | wt.% or % as stated |
| 3 | Cloud point / wax content | Onset of visible cloudiness / wax fraction. | °C / wt.% |

B  ADDITIVE PACKAGES — Route-defining fields / Numeric contribution

| Tier | Property / field | Meaning | Unit / test condition |
| --- | --- | --- | --- |
| 1 | Type / application | Package category and intended lubricant service. | Descriptive; PVL, CVL, gear, ATF, etc. |
| 1 | Claims / semantics | Claimed API, ACEA, OEM etc.; distinguish approval vs recommendation and scope. | Designation + claim type / evidence |
| 1 | SAE grades / restrictions | Documented grades, permitted base oils, exclusions and allowed combinations. | SAE grade / API group / descriptive |
| 1 | Treat rate / co-additives | Package dose by claim/grade; required VM, PPD or booster doses. | Min / max / typical wt.% |
| 1 | Published formulation | Exact supplier recipe and measured results. | Each ingredient wt.%; total 100 wt.% |
| 2 | TBN / sulfated ash | Alkalinity reserve / inorganic ash after testing. | mg KOH/g / wt.% |
| 2 | Ca, Mg, Zn, P, B, Mo, N, S | Elemental contributions of the package. | wt.% each |
| 2 | KV40 / KV100 / density | Package flow properties and mass per volume. | cSt at 40/100°C; kg/m³ at stated °C |
| 2 | Flash / pour point | High-temperature ignition / low-temperature flow indicators. | °C; record flash method |

C  ADDITIVE COMPONENTS — General / VM / PPD

| Applies to | Property / field | Meaning | Unit / test condition |
| --- | --- | --- | --- |
| All | Function / chemistry | Primary/secondary function and chemical family (e.g., ZDDP, OCP, PMA). | Descriptive |
| All | Active / carrier / dose | Active ingredient fraction, carrier identity/share and recommended treat range. | wt.% with basis; min/max/typical wt.% |
| All | Compatibility / markers | Permitted oils, co-additives, seals; relevant TBN, Ca/Mg, P/Zn or Mo. | Descriptive; marker units as reported |
| VM | VM response / SSI | Viscosity thickening at a named oil/dose; shear-stability index and post-shear behavior. | ΔKV100 cSt; SSI unitless; method/cycles |
| VM | VM cold / blend behavior | HTHS, CCS/MRV effects, gelation, dissolution/blend temperature. | mPa·s at stated °C; blend °C |
| PPD | PPD response / process | Pour-point and MRV/CCS response vs dose, wax compatibility, addition procedure. | °C / mPa·s at dose and reference oil |

Extraction rule  Never infer absent facts. Preserve source + page + revision; mark Reported / Calculated / Missing / Not applicable. A component response needs reference oil, dose and method.